## Slide 1: Study of focusing aerogels with test beams
A.Yu.Barnyakov, M.Yu.Barnyakov, V.S.Bobrovnikov, A.R.Buzykaev, V.V.Gulevich, P.V.Kasyanenko, S.A.Kononov, D.V.Korda, E.A.Kravchenko, V.N.Kudryavtsev, I.A.Kuyanov, A.P.Onuchin, I.V.Ovtin, N.A.Podgornov, V.G.Prisekin, L.I.Shekhtman, A.A.Talyshev Budker Institute of Nuclear Physics, Novosibirsk, Russia
A.F.Danilyuk Boreskov Institute of Catalysis, Novosibirsk, Russia
D.A.Finogeev, A.B.Kurepin, A.I.Reshetin, E.A.Usenko Institute of Nuclear Research RAS, Moscow, Russia
C.Degenhardt, R.Dorscheid, T.Frach, O.Muelhens, R.Schulze, B.Zwaans Philips Digital Photon Counting, Aachen, Germany
Sergey Kononov
Instrumentation for Colliding Beam Physics conference, INSTR14
February 27, 2014

## Slide 2: FARICH – Focusing Aerogel RICH
T.Iijima et al., NIM A548 (2005) 383 A.Yu.Barnyakov et al., NIM A553 (2005) 70
n=1.030 6.0mm
n=1.027 6.3mm
n=1.024 6.7mm
n=1.022 7.0mm
First sample of 4-layer aerogel by BIC
3-layer aerogel 115x115x41 mm3
Focusing aerogel improves proximity focusing design by reducing the contribution of radiator thickness into the Cherenkov angle resolution
Multi-layer monolith aerogels are produced by the Boreskov Institute of Catalysis in coop. with BINP since 2004. In 2012 we succeeded in production of continuous density gradient aerogels.
Single ring option
Multi-ring option
Notes: Идея ФАРИЧ появилась в 2004 г.
Точность измерения черенковского угла связана с точностью измерения скорости, а значит с качеством разделения частиц.

## Slide 3: FARICH projects and proposals
FARICH PID system for Super c-τ factory (BINP)
Particle ID : μ/π up to 1.7 GeV/с
~21m2 detector area (SiPM) ~106 pixels with 4 mm pitch
Belle II ARICH (talk by Yosuke Yusa)
Particle ID: π/K up to 4 GeV/c
Forward end-cap: ~3m2
Two (separate) layers of aerogel: n1= 1.045, n2= 1.055
Photon detector: HAPD (Hamamatsu)
PANDA Forward RICH (BINP)
Particle ID: π/K/p up to 10 GeV/с
3m2 detector area (MaPMTs or SiPMs)

## Slide 4: PID capability of FARICH @ Super c-τ Factory
μ momentum range for τ → μγ at Ecm=4.2GeV
μ/π
μ/π is needed for LFV search in τ→μγ.
Target sensitivity on Br(τ→μγ) ~10-9
π/K
MC simulation: MPPC&4-layer aerogel
Such PID level is not achievable with other detectors like (F)DIRC

## Slide 5: FARICH detector prototype with CPTA MRS APDs. BINP e− test beam in 2011.
Poster by V. Bobrovnikov “Extracted electron and gamma beams in BINP“
4-layer aerogel focusing at 62 mm
n1=1,050 t1=6,2mm
n2=1,041 t2=7,0mm
n3=1,035 t3=7,7mm
n4=1,030 t4=9,7mm
Size: 100x100x31mm3
Lsc(400nm) = 43mm
32 CPTA MRS APDs with active pixel size 2.1x2.1mm2

## Slide 6: Single pixel approach for aerogel characterization
Given a tracking system and enough particle statistics, a single PD pixel is enough to build the distribution of Cherenkov photons on Rch (θch).
Many pixels can be combined to improve accuracy and align the tracking system with the PD pixels
Sum of all pixels w.r.t. track position

## Slide 7: Beam test 2011 results
σr=1.1 mm – in rough agreement with MC simulation ‹Np.e. › = 13 – 2 times less than expected
4-layer aerogel (t=3cm) vs single layer aerogel (t=2cm)
Focusing effect has been observed.
σr vs channel
Np.e. vs channel
σr =1.1 mm
σr =2.1 mm

## Slide 8: Absolute PDE measurements of CPTA MRS APDs
Our measurements
CPTA data

## Slide 9: DPC: Front-end Digitization by Integration of SPAD & CMOS Electronics Philips Digital Photon Counting (PDPC)
Digital Photon Counter (DPC)
T. Frach, G. Prescher, C. Degenhardt, B. Zwaans, IEEE NSS/MIC (2010) pp.1722-1727
C. Degenhardt, T. Frach, B. Zwaans, R. de Gruyter, IEEE NSS/MIC (2010) pp.1954-1956

## Slide 10: DPC tile – PCB with densely packed 4x4 sensors (8x8 pixels)
FPGA
Clock distribution
Data collection/concentration
TDC linearization
Saturation correction
Skew correction
Flash
FPGA firmware
Configuration
Inhibit memory maps
32.6 mm
DPC3200-22-44 – 3200 cells/pixel
DPC6400-22-44 – 6396 cells/pixel

## Slide 11: First test of DPC in RICH: PDPC-FARICH prototype @ CERN PS T10, June 2012
Main objective:
  Proof of concept: full Cherenkov ring detection with a DPC array
Details:
Operation temperature is −40°C to suppress dark count rate
  Dead time is 720 ns.
  DCR(+25°C) ≈ 10 Mcps/sensor single photon detection is not feasible!
  DCR(-40°C) ≈ 100 kcps/sensor inefficiency is 7% .
2 stage cooling: LAUDA process thermostat + Peltiers.
Dry N2 constant flow to avoid condensation.

## Slide 12: PDPC-FARICH setup
Square array 20x20 cm2
DPC3200-22 sensors,
3200 cells per pixel of 3.2x3.9 mm2
3x3 modules = 6x6 tiles = 24x24 sensors = 48x48 pixels
576 timing channels
2304 amplitude channels (pixels)
3 levels of FPGA readout: tiles, modules, data collection board.
4-layer aerogel
nmax = 1.046
Thickness 37.5 mm
Focal distance 200 mm
Test conditions
Beam content: e+, μ+, π+, K+, p
Momentum: 1–6 GeV/c
Trigger: 2 sc counters 1.5x1.5 cm2 in coincidence separated by 3 m
No external tracking, particle ID, precise timing of trigger

## Slide 13: PDPC-FARICH: Ring fitting
Hit time w.r.t. fitted event time, ns
p
e, μ, π, K
P = 6 ГэВ/c
Отбор срабатываний и подгонка кольца:
Отбрасывание центральных срабатываний
Отбор в 4 нс временном окне относительно среднего времени
≥3 срабатывания
Метод максимального правдоподобия с 4 параметрами: X0, Y0, R, t0

## Slide 14: PDPC-FARICH: timing resolution and number of photoelectrons
σnarrow = 48ps
A record single photon resolution for SiPMs!
Hit time w.r.t. fitted event time, ns
‹Np.e. › = 12 (accounted for optical crosstalks)
1.7 times lower than expected
Number of hits

## Slide 15: PDPC-FARICH: Particle ID evaluation
π /K: 7.6σ @ 4 GeV/c
μ/π: 5.3σ @ 1 GeV/c
2.3 times higher than SuperB FDIRC
1.4 times higher than Belle II ARICH
2.6 times less than in initial MC simulation (with producer’s PDE)
A.Yu. Barnyakov, et al., NIM A 732 (2013) 352
Ring distribution on radius

## Slide 16: FARICH prototype #2 with CPTA MRS APDs diam 1.28 mm
60 CPTA 151, diam 1.28 mm,
noise 1-2 MHz/mm2 at room
temperature

## Slide 17: Upgraded PDPC-FARICH prototype at BINP BINP e− test beam in 2013

## Slide 18: Beam test 2013 preliminary results
Only 17 of 36 DPC tiles were functioning due to an initial failure. Still more than enough for aerogel characterization.
Each DPC pixel was electronically masked to 1x1 mm2 size (part of SPADs were disabled)
4 GEM strip chambers with 70 μm internal resolution were employed for tracking.
14 aerogel samples including ones with continuous density gradient were measured in several positions each. 7M events were acquired.
Data analysis is in progress.
“CERN” 4-layer aerogel

## Slide 19: Absolute PDE measurement of DPC
λ = 470 nm
PDE(470nm)=19±1% vs 36% according to PDPC data
PIN-diode Hamamatsu S1336-8BQ
Measurement was done at T=−30°C. No temperature dependence was studied.
DPC
Interference pattern due to chip protective SiN/SiO2 coating

## Slide 20: Continuous density gradient aerogel
To produce aerogel tiles with designed profile of gradient we modernized the method suggested by
[S.M. Jones “A method for producing gradient density aerogel”, J Sol-Gel Sci Technol. 44 (2007) 255]
We mix two pre-prepared mixtures with different content of TEOS from vessels A and B.
The mixture with designed concentration of TEOS seeps through the filter to the mould where gelation takes place.
The mould is positioned on the vertically moving table. The peristaltic pumps and moving table are controlled by a computer.

## Slide 21: Continuous density gradient aerogel
To produce aerogel tiles with designed profile of gradient we modernized the method suggested by
[S.M. Jones “A method for producing gradient density aerogel”, J Sol-Gel Sci Technol. 44 (2007) 255]
We mix two pre-prepared mixtures with different content of TEOS fed by peristaltic pumps from vessels A and B.
The mixture with designed concentration of TEOS seeps through the filter to the mould where gelation takes place.
The mould is positioned on the vertically moving table. The peristaltic pumps and moving table are controlled by a computer.
Refractive index profile along thickness

## Slide 22: Summary
Since 2011 we have done a series of beam tests with FARICH detector prototypes based on different SiPM technologies: CPTA MRS APD and Philips DPC.
Effect of focusing aerogel is clearly observed.
PS T10 at CERN we obtained π/K-separation 7.6σ at P=4 GeV/c, μ/π-separation 5.3σ at P=1 GeV/c
Number of photoelectrons is significantly lower than expected for all SiPMs.
Study of aerogels with the electron beam with fine position resolution is ongoing.

## Slide 23: DPC hierarchy in PDPC-FARICH
Module
Pixel-in-module packing density ≈70%
Tile
Pixel = 1 amplitude ch 6396 cells (DPC6400-22-44) 3200 cells (DPC3200-22-44)
Die = 1 timing ch
7.88
7.15
3.20
3.88

## Slide 24: DPC: Higher PDE than PMT is Possible
DPC3200-22-44
DPC6400-22-44
3.3V excess voltage, -20°C, randomly selected diodes
Measured one diode at a time, 50 cm slit
Parallel measurement with PIN photodiode
Transmission window not optimized yet → strong decline towards dark blue/UV
no ARC → strong interference patterns