## Slide 1: R&D of Focusing Aerogel RICH detectors
Presented by Sergey Kononov
A.Yu.Barnyakovabe, M.Yu.Barnyakovabc, K.I.Beloborodovabe, V.S.Bobrovnikovab, A.R.Buzykaevab, A.F.Danilyukbd, D.A.Finogeevf, V.V.Gulevicha, A.A.Katcinac, P.S.Kirilenkoab, S.A.Kononovabe, D.V.Kordaabe, E.A.Kravchenkoab, A.B.Kurepinf, I.A.Kuyanovabe, A.P.Onuchinabc, I.V.Ovtinabc, N.A.Podgornovabe, A.I.Reshetinf, A.A.Talyshevab, E.A.Usenkof
a Budker Institute of Nuclear Physics
b Novosibirsk State University
c Novosibirsk State Technical University
d Boreskov Institute of Catalysis SB RAS, Novosibirsk, Russia
f Institute of Nuclear Research RAS, Moscow, Russia
e FSBI NRC "Kurchatov Institute" – ITEP
Instrumentation for Colliding Beam Physics (INSTR-17)
March 2, 2017

## Slide 2: Aerogel RICH short history
Mid 1990ties – silica aerogel was proposed for use in RICH D.E. Fields et al., NIM A 349 (1994) 431 R.De Leo, et al., NIM A 401 (1997) 187
1995-200x – LHCb RICH1 with gaseous and aerogel radiator (Novosibirsk aerogel n=1.03) T. Ypsilantis, J. Seguinot, NIM A 368 (1995) 229 LHCb RICH TDR (2000) CERN LHCC 2000-037
1998 – HERMES RICH with gaseous and aerogel radiators (Matsushita aerogel n=1.03) D. Ryckbosch, NIM A 433 (1999) 98 R.De Leo, NIM A 595 (2008) 19
2003-2004 – focusing multilayer aerogel radiator was proposed to improve proximity focusing RICH P. Krizan, Aerogel RICH, talk at SuperB wokshop in Hawaii, Jan 2004 A.Yu. Barnyakov, et al., Focusing aerogel RICH, NIM A 553 (2005) 70
HERMES RICH aerogel radiator
LHCb aerogel tile
First multi-layer aerogel

## Slide 3: Quartz vs Aerogel radiators
Difference in Cherenkov angle θc for π and K
Bands – chromatic dispersion in 350-700 nm
n=1.05

## Slide 4: Focusing Aerogel RICH (FARICH)
T.Iijima et al., NIM A548 (2005) 383 A.Yu.Barnyakov et al., NIM A553 (2005) 70
n=1.030 6.0mm
n=1.027 6.3mm
n=1.024 6.7mm
n=1.022 7.0mm
First sample of 4-layer aerogel
3-layer aerogel 115x115x41 mm3
Focusing aerogel improves proximity focusing design by reducing the contribution of radiator thickness into the Cherenkov angle resolution
Multi-layer monolith aerogels have been being produced by the Boreskov Institute of Catalysis in cooperation with the Budker INP since 2004.
Notes: Идея ФАРИЧ появилась в 2004 г.
Точность измерения черенковского угла связана с точностью измерения скорости, а значит с качеством разделения частиц.

## Slide 5: FARICH-like projects and proposals
FARICH for ALICE HMPID upgrade
Belle II Aerogel RICH See talk by Luka Santelj
PANDA Forward RICH
FARICH for Super Charm-Tau factory
SuperB Forward RICH
Closed
Closed

## Slide 6: SuperB Forward RICH project (closed)
Radiator: 4- or 2-layer aerogel + NaF
PD: Photonis MCP PMTs

## Slide 7: FARICH for Super Charm-Tau Factory
μ momentum range for τ → μγ at Ecm=4.2GeV
μ/π: MC simulation MPPC & 4-layer aerogel
μ/π is required for LFV search in τ→μγ.
Target sensitivity on Br(τ→μγ) ~10-9
This PID level is not achievable with DIRC-like detectors
Proximity focusing RICH
~21 m2 photon detector area
Use SiPMs due to 1T magnetic field
~106 pixels with 4 mm pitch
4-layer or gradient aerogel radiator

## Slide 8: SiPMs in RICH applications
Pros
Excellent single photon resolution
High PDE
Sub-ns timing resolution
Immune to strong magnetic field
Very compact
Cons
High dark count rate (10-100 kHz/mm2)
Radiation induced damage (~1010 n1MeV/cm2)
S. Korpar et al., NIM A 594 (2008) 13
A.Y. Barnyakov et al., NIM A 732 (2013) 352
S. Korpar et al., NIM A 766 (2014) 107
M. Contalbrigo, NIM A 787 (2014) 224
I. Balossino et al., NIM A (2016) [doi: 10.1016/j.nima.2017.01.074]
See talk by Yuri Museinko “Advances in Solid State Photon Detectors”

## Slide 9: First tests of Novosibirsk multilayer aerogels at KEK (2005)
Tracking by 2 MWPCs
π @ 3GeV/c
KEK-PS π2 beam line
Focusing effect for single layer aerogel with non-homogenious refractive index observed
3x3 H8500 MAPMTs
Aerogel

## Slide 10: Tests of Novosibirsk multilayer aerogels at Frascati (2009)
R. De Leo et al, NIM A 617 (2010) 381 doi:10.1016/j.nima.2009.06.084
C. Arnaboldi et al, Nuclear Physics B Proceedings Supplements 197 (2009) 57 doi: 10.1016/j.nuclphysbps.2009.10.034
Frascati Beam Test Facility
8 H9500 MAPMTs
Aerogel
3-layer aerogel
Single layer aerogel
500 MeV/c e−

## Slide 11: FARICH detector prototype with CPTA MRS APDs BINP e− test beam in 2011
4-layer aerogel focusing at 62 mm
n1=1,050 t1=6,2mm
n2=1,041 t2=7,0mm
n3=1,035 t3=7,7mm
n4=1,030 t4=9,7mm
Size: 100x100x31mm3
Lsc(400nm) = 43mm
32 CPTA MRS APDs with active pixel size 2.1x2.1mm2

## Slide 12: Cherenkov ring observation with single pixels
Given a tracking system and enough particle statistics, a single PD pixel is enough to build the distribution of Cherenkov photons on Rch (θch).
Many pixels can be combined to improve accuracy and align the tracking system with the PD pixels
Sum of all pixels w.r.t. track position

## Slide 13: Focusing Aerogel beam test in Novosibirsk (2011)
σr=1.1 mm – in rough agreement with MC simulation ‹Np.e.› = 13 – 2 times less than expected
4-layer aerogel (t=3cm) vs single layer aerogel (t=2cm)
Focusing effect has been observed.
σr vs channel
Np.e. vs channel
σr =1.1 mm
σr =2.1 mm
4-layer aerogel

## Slide 14: PDPC-FARICH prototype beam test CERN PS/T10, 2012
Main objective:
  Proof of concept: full Cherenkov ring detection with a DPC array
Details:
Operation temperature is −40°C to suppress dark count rate
  Dead time is 720 ns.
  DCR(+25°C) ≈ 10 Mcps/sensor single photon detection is not feasible!
  DCR(-40°C) ≈ 100 kcps/sensor inefficiency is 7% .
2 stage cooling: LAUDA process thermostat + Peltiers.
Dry N2 constant flow to avoid condensation.

## Slide 15
p
e, μ, π, K
P = 6 GeV/c
PDPC-FARICH: Cherenkov ring

## Slide 16: PDPC-FARICH: Particle ID
π /K: 7.6σ @ 4 GeV/c
μ/π: 5.3σ @ 1 GeV/c
2.6 times less than in initial MC simulation (with producer’s PDE and ideal aerogel)
A.Yu. Barnyakov, et al., NIM A 732 (2013) 352
Ring distribution on radius

## Slide 17: Refractive index of 4-layer aerogel tested at CERN
X-ray scan

## Slide 18: PDPC-FARICH: timing resolution and number of photoelectrons
σnarrow = 48ps
Excellent single photon resolution for SiPMs
Hit time w.r.t. fitted event time, ns
‹Np.e. › = 12 (accounted for optical crosstalks)
1.7 times lower than expected due to overevaluated DPC PDE by producer’s data
Number of hits

## Slide 19: PANDA Forward RICH
Photon Detector
Hamamatsu H12700 MaPMT
flat panel,
8x8 anode pixels of 6mm size
87% active area ratio
Bialkali photocathode
Gain: 1.5∙106
Good single p.e. amp resolution
Robust
Long lifetime
Works in the mag. field 25G (stray field of the dipole)
Radiator
Focusing 2- or 3-layer aerogel
40 mm thick
No gaseous radiator
Mirrors
Flat segments
Float glass substrate 2 mm thick
Al+SiO2 coating, R≥90%
Light-weight Al or carbon fiber support
Simplicity of production and positioning
PD
mirrors
aerogel

## Slide 20: Readout options for PANDA FRICH
Hamamatsu H12700B
May be influenced by stray magnetic field
Needs FEE
Digital Photon Counter
720 ns sensor dead time
Needs cooling
Not radiation hard (lifetime ~1 year in PANDA FRICH w/o neutron shielding)

## Slide 21: DPC radiation hardness study
4∙109 n1MeV/cm2
2 times drop
PDE degradation due to DCR increase
Effect of radiative damage on DCR
COSY PS in IKP FZ Jülich
protons @ 800 MeV/c
DPC tiles cooled to −18°C

## Slide 22: PANDA FRICH performance (MC sim)
Efficiency of reconstruction

## Slide 23: Continuous density gradient aerogel
To produce aerogel tiles with designed profile of gradient we modernized the method suggested by
[S.M. Jones “A method for producing gradient density aerogel”, J Sol-Gel Sci Technol. 44 (2007) 255]
We mix two pre-prepared mixtures with different content of TEOS fed by peristaltic pumps from vessels A and B.
The mixture with designed concentration of TEOS seeps through the filter to the mould where gelation takes place.
The mould is positioned on the vertically moving table. The peristaltic pumps and moving table are controlled by a computer.
Refractive index profile along thickness

## Slide 24: Conclusion
FARICH R&D was reviewed
Focusing aerogel is a perspective Cherenkov radiator for few-GeV momenta and proximity focusing design
Problems with production of monolithic multilayer aerogels with refractive index profile conforming to designed one
Continuous density gradient aerogels and stacked aerogel tiles are considered as alternatives

## Slide 25: Thank you for your attention!