## Slide 1: archPbMoO4 scintillating bolometers as detectors to search for neutrinoless double beta decay of 100Mo
1st March 2017
Serge Nagorny
INFN – Gran Sasso Science Institute, L`Aquila, Italy
on behalf of the CUPID-0 collaboration

## Slide 2
Double Beta Decay (DBD)

## Slide 3: DBD active nuclei in the nature

## Slide 4: Which nuclide is the best for such search?
Environmental gamma background of 238U and 232Th chains
2615 keV
48Ca
82Se
96Zr
100Mo
116Cd
150Nd
from experimental point of view
76Ge
130Te

## Slide 5
Development of TeO2 bolometers
TeO2 is wide used acousto-optic material with market of tens MEuro/year and well-developed technology of production

## Slide 6
a future ton-scale bolometric neutrinoless double beta decay experiment with improved sensitivity, based on the experience and expertise learned in CUORE
The CUPID goal is the use of the unique CUORE infrastructure @ LNGS, once CUORE completes operation, as well as using of upgraded detector technology in order to reach higher experimental sensitivity
New detector technologies (background rejection or surface events ID)
Isotopic enrichment
New purification and crystallization procedures
Stricter materials selection
CUORE Upgrade with Particle Identification

## Slide 7
Czochralski

## Slide 8
Working principle of scintillating bolometers

## Slide 9: CUPID-0
Demonstrator array of enriched Zn82Se scintillating bolometers
Total enriched 82Se isotope mass is 7 kg
Expect background index @ROI < 10-3 c/(keVkgy)

## Slide 10: Some crucial detector parameters
Radiopurity (internal background)
Light Yield
FWHM
PSD
High content of isotope of interest
Well-developed technology of crystals production

## Slide 11
2007, Moscow
2012, Moscow
2004, Moscow
2003, Korea
2005, Ukraine
CaMoO4
2015, Novosibirsk

## Slide 12: ZnMoO4
2008, Moscow
2009, Kharkov
2012, Kharkov
2012, Novosibirsk

## Slide 13: Li2MoO4
2015, Novosibirsk
2014, Kharkov
2004, Moscow

## Slide 14: Mo-containing crystals
CaMoO4
ZnMoO4
Li2MoO4
……
PbMoO4 crystal is one of the most efficient materials used for acousto-optic devices (modulators, deflectors and phase-shifters) which possess a low optical losses, high optical homogeneity, high stability to laser radiation
The same like in case of the TeO2 crystals!!!
Market demands & developed technology
No other applications
No other applications
No other applications
What about PbMoO4?

## Slide 15: archPbMoO4: conventional Czochralski technique
archPbMoO4 boule
Total mass is 175 g
20×90 mm
Highly purified archaeological lead, > 99.999%
Re-crystallized MoO3 powder, > 99.99%
Conventional Czochralski technique
Production yield is about of 50%
57 g
20×25 mm
Light detector
archPbMoO4
Low-background measurements
LNGS

## Slide 16: archPbMoO4: Light Yield @ low temperature
 10 times

## Slide 17: archPbMoO4: Light-vs-Heat scatter plot
 + 

 + 

Well separated population of different type of events

## Slide 18: archPbMoO4: pusle-shape discrimination
beta/gammas
Shape parameter, a.u.
Energy, MeV
alphas

## Slide 19: archPbMoO4: alpha spectrum
FWHM = 9 keV @ 4970 keV (226Ra)
FWHM = 5 keV @ 1462 keV (40K)
Excellent energy resolution!

## Slide 20: archPbMoO4: internal alpha contamination
Chain | Nuclide | Activity, mBq/kg
232Th | 232Th | 10±7
 | 228Th | 99±9
 | 224Ra | 86±8
 | 220Rn | 21±5
 | 212Bi | 49±7
238U | 238U | 38±6
 | 234U | 98±9
 | 230Th | 13±3
 | 226Ra | 2310±42
 | 222Rn | 2370±42
 | 218Po | 2340±42
 | 210Po | 266±16
235U | 235U | 14±3
 | 227Th | 17±4
 | 223Ra | 30±5
 | 219Rn | 5±2
 | 211Bi | 30±5
…but we have explanation
based on our experience
with ZnSe crystal
HUGE!!!

## Slide 21: Separation process of ZnSe sample (15/01/2013)
Piece of ceramic
m = 0.285 g
226Ra & daugthers (about 0.2 kBq/kg)
40K nuclide (1 kBq/kg)
High contamination observed in archPbMoO4 crystal is caused by incident during the growth process, when a small piece of ceramic (0.01-0.05 g) fall dawn to the melt, but NOT by the properties of the material itself

## Slide 22
Pt-crucible
conventional Czochralski
LTG Czochralski
Notes: 22

## Slide 23
PbMoO4: at Novosibirsk
Presently used natural Mo & Pb
No problems in crystals growth
Yellow color is due to the low purity of initial materials
First trial with archaeological lead will start this week!

## Slide 24: New batch of archaeological Lead @ LNGS
After purification by double stage
vacuum distillation
Sn = 5.2 ppm
Sb = 2.6 ppm
others on tens ppb level
2319.2 g
Reduction
of impurities level
in more than 10 times
Yield  95%

## Slide 25: Some useful parameters
 | Li2MoO4 | ZnMoO4 | PbMoO4 | CaMoO4
LY, keV/MeV | 0.13 | 0.26 | 1.2 | 0.71.4
LY, keV/MeV | 0.43 | 1.54 | 5.5 | 3.56.8
FWHM, keV @2.6 MeV | 5 | 6.8 | < 5 | 9
PSD | yes | yes | yes | yes
Particle identification | yes | yes | yes | yes
 (Mo), % | 55 | 43 | 26 | 48
N(Mo)1023 in 1 cm3 | 0.105 | 0.115 | 0.112 | 0.131
Background level | low | low | low ??? | high
Hygroscopicity | yes | no | no | no

## Slide 26: archPbMoO4: SUMMARY
archPbMoO4 crystal produced from the archaeological lead demonstrates excellent performance as a scintillating bolometer
Crystal’s radiopurity soon will be re-checked with new crystals produced by LTG Czochralski method
archPbMoO4 crystals is promising material for a future ton-scale bolometric DBD experiment with improved sensitivity

## Slide 28: … just visiting a friend in Sicily
…it is about of 400-500 kg of Roman lead!
06/09/2016

## Slide 29: …or we can go deep underwater to discover a sunken ships and to excavate the Roman lead
with C-Explorer 3 submarine…

## Slide 31: From the crystal producer viewpoint
Well-developed technology of detector production means:
Developed technology of purification of initials reagents
Developed technology of large volume crystal production
Possibility to fast scalability of growth process
High yield of good crystals
Developed technology of recovery of the rest materials after the growth
Easy handling/machining
Other applications of this compound, or market demands exactly on such large single crystals
NO RISCKS for investments in such R&D or production,
and expected profit in the future