## Slide 1: Pulse-shape discrimination with Cs2HfCl6 crystal
C. Cardenas1,2, A. Burger1,2, E. Rowe1, B. Goodwin1,
M. Groza1, M. Laubenstein3, S. Nagorny3,4
1Department of Life and Physical Sciences, Fisk University, Nashville, TN USA
2Department of Physics and Astronomy, Vanderbilt University, Nashville, TN USA
3INFN – Laboratori Nazionali del Gran Sasso, Assergi, Italy
4INFN – Gran Sasso Scientific Institute, L’Aquila, Italy
INSTR-2017, 3 March 2017

## Slide 2: Cs2HfCl6 (CHC) crystal sample grown at Fisk University
Self-activated scintillator
Nonhygroscopic
High Z (58)
Moderate density
High light yield (54000 photons/MeV)
Energy resolution 3.3% @ 662 keV
Good linearity
Peak of emission wavelength at 400 nm
Decay time about of
Energy resolution of 3.3% at 662 keV
Hf content is 25%
12.15 g
24×7.9 mm
First scintillator containing a high concentration of Hf !

## Slide 3: How we can use it?
Transition energy, keV
Atomic number, A
Q  0
Т1/2  1011 y
Т1/2  1011 y
difficult to detect
easy to detect
Just one experiment
Low sensitivity
Contradiction with theory
T1/2 = (3-7)×1016 y
174Hf alpha decay
Q = 2497 keV
T1/2 = 2×1015 y
Must be re-measured
with a new technique

## Slide 4: Experimental Setup for crystal characterization
CHC
Pre-Amplifier
Shaping
Amplifier
MCA
Digitizer
Optical grease
PMT
Dark box
 source
Reflector

## Slide 5: Calibration measurements
137Cs source, 662 keV gamma
241Am alpha source, 3 mm collimator
Events considered in further pulse-shape analysis
5.3%
23.4%
Notes: Need to fit the 662 keV peak with exp mod. Gaussian function, so that the peaks of the data and fit function match!!!
Pure 662 keV events considered in further pulse-shape analysis

## Slide 6: Quenching Factor for alpha particles
Energy scale of detector was calibrated with 137Cs gamma source
Typically crystal scintillator have a
different response for different particles type
QF is very important experimental parameter that allows us to understand where alpha peaks should appear in the gamma calibrated energy spectrum
23.4%
5155 keV is real alpha energy
Actual position of alpha peak
@ 1465.1 keV in gamma scale
Notes: In alpha particle spectroscopy, the quenching factor is an important characteristic of detector that allows us to understand where our alpha peaks should appear in the gamma calibrated energy spectrum. Quenching factor is dependent on the energy of alpha particle. For more precise characterization of our detector, one must measure this factor in respect with different alpha particle energy. With a preference to use the internal alpha source of our crystal

## Slide 7: Average pulses
Type of irradiation | Decay constants (s) and relative intensities |  |  | 
 | 1 (A1) | 2 (A2) | 3 (A3) | 4 (A4)
gamma | 10.4 (27.1) | 4.1 (66.4) | 0.18 (1.0) | 0.84 (5.5)
alpha | 6.3 (56.0) | 2.5 (34.2) | 0.12 (1.7) | 0.56 (8.0)
gamma
alpha

## Slide 8: Comparison of average pulses
Difference in pulse shape resulting in the particle discrimination ability
gamma
alpha
Mean Time Method
Optimal Filter Method

## Slide 9: Pulse Shape Discrimination with OF
Gamma | 
Mean | - 0.96
Sigma | 0.034
Alpha | 
Mean | 0.55
Sigma | 0.023

## Slide 10: Pulse Shape Discrimination with MT
Gamma | 
Mean | 49.7 μs
Sigma | 0.9 μs
Alpha | 
Mean | 42.2 μs
Sigma | 0.6 μs

## Slide 11: Decay-time vs Energy scatter plot
Gamma, 662 keV of 137Cs
Alpha, 5.15 MeV of 241Am

## Slide 12: Gran Sasso Underground Laboratory
Average depth  3650 m w.e.
Muon flux  2.6×10-8 μ/s/cm2
Neutrons < 10 MeV: 4×10-6 n/s/cm2
Gamma < 3 MeV: 0.73 γ/s/cm2

## Slide 13
10-4
10-3
10-2
10-1
100
101
102
103
Normalised counting rate [d-1 keV-1 kg-1]
Energy [keV]
0
1500
500
1000
2000
2500
3000
Above ground
Underground

## Slide 14: Schematic view of the HPGe detector “Ge-Cris”
Pb, 30 cm
Cu, 5-10 cm
HP Ge
408 cm3
CHC crystal
12.15 g
Plexiglas box
Radon free N2 gas
FWHM = 1.8 keV @ 1332 keV
CsCl, HfCl3 and HfCl3 dist. samples will be measured after CHC crystal

## Slide 15
132Cs
667 keV
134Cs
795 keV
137Cs
662 keV
134Cs
605 keV
40K
1462 keV
137Cs
662 keV
Bkg
CHC
Bkg
CHC
Energy, keV
Energy, keV
Counts/1 keV
Counts/1 keV
Internal radioactive contamination
measured with 12.15 g CHC crystal on HPGe detector (408 cm3) within 494 hours
Main contamination comes from artificial 137Cs and cosmogenic 132,134Cs nuclides

## Slide 16
Internal radioactive contamination
12.15 g Cs2HfCl6 crystal, HP Ge detector (408 cm3) , 493.6 hours
Chain | Nuclide | Activity, mBq/kg
232Th | 228Ra | < 12
 | 228Th | < 6.3
238U | 226Ra | < 8.6
 | 234Th | < 3.7
 | 234mPa | < 0.31
235U | 235U | < 26
 | 40K | < 0.18
 | 60Co | < 19
 | 132Cs | 258
 | 134Cs | 526
 | 137Cs | 83090
 | 181Hf | 140.7

## Slide 17: Summary
Pulse shape for alpha and gamma particles is different in CHC crystal
Pulses are well fitted by sum of four exp, and its amplitudes and times were determined
Excellent particle discrimination was achieved both with Optimal filter method and Mean time analysis
PSD for CHC crystal will be used for background suppression in experiment to search for rare decays of Hf isotopes
Notes: Measured

## Slide 19
Element | CsCl | HfCl3 | HfCl3 dist*3 | Cs2HfCl6 crystal
La | 8,7 | 2627 | 555 | 132
Ce | <5 | <5 | <5 | 19
Pr | <5 | <1 | <1 | 5,8
Nd | <10 | <10 | <10 | <12
Sm | <15 | <15 | <15 | <15
Eu | <3 | 33 | 25 | 130
Gd | <5 | <15 | <5 | <35
Tb | 11 | <2 | <2 | 6
Dy | 2,2 | <1 | <1 | 16
Ho | <4 | 250 | 204 | <25
Er | <2 | <2 | <2 | <2
Tm | <3 | <2 | <2 | <2
Yb | <5 | <100 | <100 | <50
Lu | <10 | <500 | <500 | <300
Ta | <3 | <8000 | <8000 | <4000
W | <1000 | <1000 | <1000 | <200
Re | <2 | <15 | <15 | <10
Os | <5 | <20 | <20 | <15
Ir | <2 | <4000 | <4000 | <2000
Pt | <2 | <100000 | <100000 | <40000
Tl | <55 | <4 | <4 | <15
Bi | <3 | <2000 | <2000 | <1000
Th | <0,5 | <1 | <1 | <0,5
U | <0,5 | 3200 | 267 | <0,5
Chemical impurities
measured by ICP-MS, expressed in ppb units

## Slide 20
Element | Concentration, ppb | Dangerous isotope | Q, MeV | Number of expected events in 2 weeks | Number of expected events in 4 weeks
Nd | < 12 | 144Nd | 1.910 | < 1.710-3 | < 3.410-3
Sm | < 15 | 147Sm | 2.310 | < 27.8 | < 55.6
 |  | 148Sm | 1.986 | < 3.210-4 | < 6.410-4
Eu | 130 | 151Eu | 1.949 | 1.710-5 | 3.410-5
Gd | < 35 | 152Gd | 2.206 | < 8.110-4 | < 1.610-3
W | < 200 | 180W | 2.516 | < 1.410-7 | < 2.810-7
Os | < 15 | 184Os | 2.966 | < 3.110-5 | < 6.210-5
 |  | 186Os | 2.816 | < 1.210-4 | < 2.410-4
Pt | < 40000 | 190Pt | 3.243 | < 7.45 | < 14.9
Bi | < 1000 | 209Bi | 3.137 | < 5.010-5 | < 1.010-4
Dangerous radioactive contamination
in 12.15 g Cs2HfCl6 crystal
during 340/680 hours
of background measurements

## Slide 21: Previous experiment: MacFarlane (1961)
Counting gas composition
94% argon, 5% ethylene, 1% nitrogen
Surface lab
Passive shield
Active shield
No PSD
About 40 days data taking
100 mg scale samples mass
Enriched 174Hf to 56%
FWHM = 4% @ 2.3 MeV
Bkg (1-3 MeV) = 9 count/h
174HfO2 samle
Notes: Optimum counting conditions were not realized at the time of Hafnium measurement. Resolution of the alpha peak is poor.

## Slide 22
174HfO2 + Sm2O3
alpha 147Sm @ 2.3 MeV
Previous experiment: MacFarlane (1961)
174HfO2 + 210Po
alpha 210Po @ 5.3 MeV
Low statistics
Low signal to background ratio
174Hf
174Hf

## Slide 23: Scintillating detector
Copper box (5 mm)
Passive shield (10-20 cm of Pb)
Underground lab (LNGS)
Plastic scintillator
CHC
Active light guide
PbWO4 crystal
SiPM array
Teflon support

## Slide 24: Scintillating bolometer
During particle interaction in the crystal a fraction of the deposited energy is converted into scintillation. Combining the crystal with cryogenic light detector allows to simultaneous measurement of the energy deposited in crystal (H) and produced scintillation (L)
Simultaneous and independent, double readout of heat and scintillation light leads to an effective discrimination of e/ from  events by the different L/H ratio
Light
Heat
e/ events
 events

## Slide 25: What we suppose to observe?
m (Cs2HfCl6) = 12.154 g
N (Hf) = 11.161021 atoms
i.a. (174Hf) = 0.16%
N(174Hf) = 1.791019 atoms
t = 2 weeks = 0.03833 y
 = 100%
S = ln 2    t  N(174Hf) / T1/2 = 15 events (theor T1/2 = 31016 y)
238 events (exp T1/2 = 21015 y)

## Slide 26
Experimental data are
coming soon!